SECTION 32 14 13.19 CONCRETE GRID PAVEMENTS

(1995 MasterFormat Section 02795)

Note: This guide specification is for concrete grid units placed on a sand bedding course over a compacted dense-graded aggregate base.  The text allows an option of topsoil and grass in the grid openings over bedding sand.  This specification is for limited vehicular applications such as access roads and emergency fire lanes, as well as intermittently used overflow parking areas. This text must be edited to suit specific project requirements for projects. This Section includes the term “Architect.” Edit this term as necessary to identify the design professional in the General Conditions of the Contract.

PART 1 GENERAL

1.01 SUMMARY

A. Section includes:

1. Concrete grid units.

2. Bedding sand.

3. Edge restraints.

4. Geotextiles.

5. Topsoil and grass for the grid openings.

B. Related Sections:

1. Section [______]: Curbs and drains.

2. Section [______]: Dense-graded aggregate base.

1.02 REFERENCES

1. ASTM C 33, Specification for Concrete Aggregates.

2. ASTM C 136, Method for Sieve Analysis for Fine and Coarse Aggregate.

3. ASTM C 140, Standard Test Methods of Sampling and Testing Concrete Masonry Units.

4. ASTM C 979, Standard Specification for Pigments for Integrally Colored Concrete.

Tech Spec 8—Concrete Grid Pavements 9 Tech Spec 8—Concrete Grid Pavements

5. ASTM C 1319, Standard Specification for Concrete Grid Paving Units.

6. ASTM D 698, Standard Test Method for Laboratory Compaction Characteristics of Soil Using Standard Effort

7. ASTM D1557 - 07 Standard Test Methods for Laboratory Compaction Characteristics of Soil Using Modified Effort.

8. ASTM D 2940, Standard Specification for Graded Aggregate Material for Bases or Subbases for Highways or Airports.

9. ASTM D 5268, Specification for Topsoil Used for Landscaping Purposes.

10. Canadian Standards Association (CSA) 1. CSA A23.1, Concrete Materials and Methods of Concrete Construction

11. Interlocking Concrete Pavement Institute (ICPI),  Tech Spec technical bulletins.

1.03 SUBMITTALS

A. In accordance with Conditions of the Contract and Division 1 Submittal Procedures Section.

B. Manufacturer’s drawings and details: Indicate perimeter conditions, relationship to adjoining materials and assemblies, expansion and control joints, paving slab [layout,] [patterns,] [color arrangement,] installation [and setting] details.

C. Sieve analysis per ASTM C 136 for grading of bedding and base materials.

D. Source and content of topsoil and grass seed [sod].

E. Concrete grid units:

1. One representative full-size sample of grid unit, thickness, color, expected in the finished installation.

2. Accepted samples become the standard of acceptance for the work.

3. Test results from an independent testing laboratory for strength compliance  requirements to ASTM C39.

4. Manufacturer’s catalog literature, installation instructions, and material safety data sheets for the safe handling of the specified materials and products.

1.04 QUALITY ASSURANCE

A. Paving Subcontractor Qualifications:

1. Engage an experienced installer who has successfully completed grid pavement installations similar in design, material, and extent indicated for this Project.

2. Hold a current certificate from the Interlocking Concrete Pavement Institute Concrete Paver Installer Certification program.

1.05 DELIVERY, STORAGE, AND HANDLING

A. General: Comply with Division 1 Product Requirement Section

B. Deliver concrete grid units to the site in steel banded, plastic banded, or plastic wrapped packaging capable of transfer by forklift or clamp lift. Unload grids at job site in such a manner that no damage occurs to the product or existing construction.

C. Cover sand with waterproof covering to prevent exposure to rainfall or removal by wind. Secure the covering in place.

D. Coordinate delivery and paving schedule to minimize interference with normal use of buildings adjacent to paving.

1.06 ENVIRONMENTAL CONDITIONS

A. Do not install bedding materials or grid units during heavy rain or snowfall.

B. Do not install bedding materials and grid units over frozen base materials.

C. Do not install frozen bedding materials.

1.07 GRID PAVER MAINTENANCE MATERIALS:

A. Supply Checker Block in unopened pallets with contents labeled. Store where directed.

PART 2 PRODUCTS

2.01 CONCRETE GRID UNITS

A. Checker Block - Manufacturer:  Hastings Pavement Company, LLC. DBA
Hastings Architectural & Ornamental Concrete
200 Henry Street
Lindenhurst, NY 11757

Contact: Kevin Earley, 631-774-6431

B. Color: Natural  - stock color

C. Size: 24 inches x 24 inches x 4 inches thick

D. Reinforcement: 6”/6” x 6 gauge welded wire

E. Minimum Average Compressive Strength: 5,000 psi at 28-days per ASTM C-39

2.02 PRODUCT SUBSTITUTIONS

A. No substitutions permitted.

2.03 BEDDING MATERIALS

A. General – Sieved per ASTM C 136.

B. Bedding Sand

Note: The type of sand used for bedding is often called concrete sand. Sands vary regionally. Contact contractors local to the project and confirm sand successfully used in previous similar applications. Bedding sand is not used in ditch liner applications, slope protection, riparian stabilization or with boat ramps constructed with concrete grid units.

1. Washed, clean, hard, durable crushed gravel or stone, free from shale, clay, friable materials, organic matter, frozen lumps, and other deleterious substances.

2. Conforming to the grading requirements in Table 1 below.

3. Do not use limestone screenings.

Table 1

2.04 BASE MATERIALS

Note: Local, state or provincial standards for aggregate base materials for roads should be used for the gradation and quality of dense graded aggregate base materials under concrete grid pavements. If no standards exist, follow ASTM D 2940, Standard Specification for Graded Aggregate Material for Bases or Subbases for Highways or Airports. The gradation for base material from this standard is based on ASTM D2940,  below. This material should be compacted to a minimum of 95% standard Proctor density.

2.05 FILL MATERIALS FOR GRID OPENINGS

A. Topsoil: Conform to ASTM D 5268.

Note: Consult with local turf grass specialists for recommendations on grass seed mixture or sod materials.

B. Grass seed [Sod]: [mixture and source].

2.06ACCESSORIES

A. Provide accessory materials as follows:

1. Geotextile separation fabric material :Strata SW200

B. Optional edge restraints installed around the perimeter of all concrete grid paving unit areas as follows:

1. Material: [Plastic] [Concrete] [Aluminum] [Steel] [Precast concrete] [Cut stone] [none].

PART 3 EXECUTION

3.01 EXAMINATION

A. Acceptance of site verification conditions:

1. Contractor shall inspect, accept and verify in writing to the grid installation subcontractor that site conditions meet specifications for the following items prior to installation of bedding materials and concrete grid units:

a. Verify that drainage and subgrade preparation, compacted density and elevations conform to specified requirements.

b. Verify that geotextiles, if applicable, have been placed according to drawing and specifications.

c. Verify that base materials, thickness, compacted density,  surface tolerances and elevations conform to specified requirements.

d. Provide written density test results for the soil subgrade, base materials to the Owner, Contractor, and grid installation subcontractor.

2. Do not proceed with installation of bedding materials and concrete grids until [subgrade soil and] base conditions are corrected by the Contractor or designated subcontractor.

3.02 PREPARATION

A. Verify that base is dry, certified by Contractor as meeting material, installation and grade specifications are ready to support sand,  grids and imposed loads.

B. Edge Restraint Preparation:

1. If required, install edge restraints per the drawings and manufacturer’s recommendations at the indicated elevations.

2. Mount directly to finished base. Do not install on bedding sand.

3. The minimum distance from the outside edge of the base to the spikes shall be equal to the thickness of the base.

3.03 INSTALLATION

Note: Stabilization of the subgrade and/or base material may be necessary with weak or saturated subgrade soils.

Local aggregate base materials  typical to those used for highway flexible pavements are recommended, or those conforming to ASTM D 2940.   Mechanical tampers are recommended for compaction of soil subgrade and aggregate base in areas not accessible to large compaction equipment. Such areas can include that around lamp standards, utility structures, building edges, curbs, tree wells and other protrusions. The recommended base surface tolerance should be ±3/8 in. (±10 mm) over a 10 ft. (3 m) straight edge.  The elevations and surface tolerance of the aggregate base determine the final surface elevations of concrete grids. The installation contractor cannot correct deficiencies in the base surface with additional bedding materials. Therefore, the surface elevations of the base should be checked and accepted by the General Contractor or designated party, with written certification to the paving subcontractor prior to placing bedding materials and concrete grids.

A. Compact soil subgrade to 95% standard Proctor density per ASTM D 698.

B. Install a minimum of 8 in. of compacted (95% standard Proctor density)  dense-graded base course, or greater thickness based on the project engineer’s requirements.

C. Spread the 1”  bedding sand layer evenly over the compacted,  base course and screed uniformly.

D. Ensure the grid units are free from foreign materials before installation.

E. Lay the grid units on the bedding sand in the pattern  shown on the drawings. Maintain straight joint lines.

F. Joints between the grids shall be maintained so that units do not touch but not exceed 3⁄16 in. (5 mm).

G. Ensure that grid pavers are seated and leveled with roller compactor or static roller drum.

H. Use tie rods to anchor units on slopes steeper than 3:1.

I. Sweep top soil into the joints and openings until full.

J. Broadcast grass seed at the rate recommended by seed source.  Place sod plugs into openings.  Add topsoil to the surface to cover the seeds.

L. Remove excess topsoil on surface when the job is complete.

M. Distribute straw covering to protect germinating grass seed or sod. Water entire area. Do not traffic pavement for 30 days,  if seeded.

3.05 FIELD QUALITY CONTROL

A. Check final elevations for conformance to the drawings. Allow 1⁄8 to 1⁄4 in. (3 to 6 mm) above specified surface elevations to compensate for minor settlement.

B. The final surface tolerance from grade elevations shall not deviate more than ± 3 ⁄8 in. (10 mm) over a 10 ft (3 m) straightedge.

C. The surface elevation of grid units shall be 1⁄8 to 1⁄4 in. (3 to 6 mm) above adjacent drainage inlets, concrete collars or channels.

D. Lippage: No greater than 1⁄8 in. (3 mm) difference in height between adjacent grid units.

3.06 PROTECTION

A. After work in the section is complete, the Contractor shall be responsible for protecting work from damage due to subsequent construction activity on the site.

END OF SECTION